## Slide 1: Recent Advances in the PAOFLOW Method—Electronic, Transport and Optical Properties of Real Materials from Projections on Atomic Orbital Bases Marco Buongiorno Nardelli University of North Texas and Santa Fe Institute

## Slide 2: Localized orbitals

## Slide 3: Localized basis sets
Chemical interpretation of the wavefunction
Simple connection with plane-waves via Fourier transforms:
  Construction of model Hamiltonians (e.g. strongly correlated systems)
  Band structure interpolation
  Transport properties
  Many more…
Bloch states (plane waves)
Localized states (i.e. atomic orbitals)

## Slide 4: Wannier functions
A convenient localized basis set.
Maximal localization: Unique basis set
Not straightforward (what projectors and how many?)
Internal iterative procedure for disentangling bands (e.g in metals)
  Energy window?
  Intractable for large number of bands
Bloch
Wannier
N. Marzari et. al. Rev. Mod. Phys. 84, 1419 (2012)

## Slide 5: Localized basis sets
Chemical interpretation of the wavefunction
Simple connection with plane-waves via Fourier transforms:
  Construction of model Hamiltonians (e.g. strongly correlated systems)
  Band structure interpolation
  Transport properties
  Many more…
Bloch states (plane waves)
Localized states (i.e. atomic orbitals)

## Slide 6: The PAOFLOW method

## Slide 7: Pseudo-atomic orbitals (PAO)
Readily available from pseudo-potentials:
Connection to Bloch states (i.e Kohn-Sham states from DFT) via a simple projection -- typically done to obtain Projected Density of States (PDOS):
We assume the basis is orthonormal
Silicon
a
a

## Slide 8: Density matrix
Lowdin Charges:
Atom # 1: total charge = 3.9897, s = 0.9061,
Atom # 1: total charge = 3.9897, p = 2.3837, pz= 0.7946, px= 0.7946, py= 0.7946,
Atom # 1: total charge = 3.9897, d = 0.6981, dz2= 0.0861, dxz= 0.1753, dyz= 0.1753, dx2-y2= 0.0861, dxy= 0.1753,
Atom # 1: total charge = 3.9897, f = 0.0018, fz3= 0.0003, fxz2= 0.0002, fyz2= 0.0002, fzx2-zy2= 0.0002, fxyz= 0.0003, fx3-3xy2= 0.0003, f3yx2-y3= 0.0003,
Atom # 2: total charge = 3.9897, s = 0.9061,
Atom # 2: total charge = 3.9897, p = 2.3837, pz= 0.7946, px= 0.7946, py= 0.7946,
Atom # 2: total charge = 3.9897, d = 0.6981, dz2= 0.0861, dxz= 0.1753, dyz= 0.1753, dx2-y2= 0.0861, dxy= 0.1753,
Atom # 2: total charge = 3.9897, f = 0.0018, fz3= 0.0003, fxz2= 0.0002, fyz2= 0.0002, fzx2-zy2= 0.0002, fxyz= 0.0003, fx3-3xy2= 0.0003, f3yx2-y3= 0.0003,
Spilling Parameter: 0.0026

## Slide 9: Pseudo-atomic orbitals (PAO)
Readily available from pseudo-potentials:
KS eigenvalues
LCAO
Hamiltonian
Si (2s22p2 basis set): 8 atomic orbitals
Valence bands reproduced to high accuracy
Conduction bands deviate strongly from KS eigenvalues.
L. A. Agapito et. al. Phys. Rev. B 88, 165127 (2013)
Connection to Bloch states (i.e Kohn-Sham states from DFT) via a simple projection -- typically done to obtain Projected Density of States (PDOS):

## Slide 10: Projectability of bands
LCAO band structure with spd basis set.
  Some low energy conduction bands improve.
  A set of null eigenvalues are inserted
Projectability:
High projectability bands (i.e. Pn ≈ 1) yield accurate LCAO band structure.
Low projectability bands (i.e. Pn << 1) yield poor LCAO bands and lead to null eigenstates.

## Slide 11: Accurate PAO Hamiltonians
bands
plane
waves
atomic
orbitals
GOOD
projectability
BAD
projectability
11

## Slide 12
12
Exclude the bad projectability states from the set of bands to be represented (filtering) – orthogonal projection
Introduces a spurious null space that must be eliminated
Shift by a fixed energy outside of the region of good projectability bands
(shifting)

## Slide 13: Accurate PAO Hamiltonians
13

## Slide 14: Accurate PAO Hamiltonians
Effective description of entangled bands in metals
Mo
Cu
projections
Wannier functions

## Slide 15: pip install paoflow

## Slide 21: K-point interpolation
21
Convergence of multi-valley bands as the electronic origin of high thermoelectric performance in CoSb3 skutterudites, Y. Tang, Z.M. Gibbs, L.A. Agapito, G. Li, H. Kim, M. Buongiorno Nardelli, S. Curtarolo and G.J. Snyder

## Slide 24: Increase the basis set

## Slide 29
Construction of PAO Hamiltonians from the DFT wavefunctions onto pseudo atomic orbitals
Construction of PAO Hamiltonians from analytical tight binding models
Hamiltonian data for further processing (ACBN0, PAOtransport, etc.)
External fields and non scf ACBN0 correction
Spin orbit correction of non SO calculations
Bands along standard paths in the BZ
Real space electronic charge density
Interpolation of Hamiltonians on arbitrary Monkhorst and Pack k-meshes
Adaptive smearing for BZ and Fermi surface integration
Density of states (and projected DOS)
Fermi surfaces and spin textures
Boltzmann transport (conductivity, Seebeck coefficient, electronic contribution to thermal conductivity
dielectric function (absorption coefficients and EELS)
Berry curvature and anomalous Hall conductivity (including magnetic circular dichroism spectra)
spin Berry curvature and spin Hall conductivity (including spin circular dichroism spectra)
Band topology (Z2 invariants, Berry and spin Berry curvature along standard paths in BZ, critical points
PAOFLOW capabilities

## Slide 30: Some more advanced applications

## Slide 31: Berry curvature and Anomalous Hall conductivity: Fe
Berry curvature from Kubo formula:
Anomalous Hall conductivity:

## Slide 32: Spin Hall conductivity

## Slide 38
MoTe2: A Type-II Weyl Topological Metal
Wang et al., 10.1103/PhysRevLett.117.056805
z2pack.ethz.ch/doc/2.1/index.html
Topological invariants

## Slide 39
Nodal chain and Weyl points in HfC